CALCITE / CALCIUM CARBONATE

GCC Export from India  ·  Coated GCC & PCC Import (Vietnam/Malaysia/Egypt) for Indian Industry  ·  Dual Business

## Section 1 — Hero content

Calcite / Calcium Carbonate — GCC Exported from India · Coated GCC & PCC Imported for Indian Industry

Sub-headline: CaCO₃ ≥97–99%  ·  GCC uncoated & stearic acid coated  ·  PCC scalenohedral & rhombohedral  ·  100 mesh to nano grades  ·  India export to Nepal/Bangladesh/Russia  ·  Import from Vietnam/Malaysia/Egypt

Two CTAs:

- "Enquire for Supply" — Indian buyers (coated GCC/PCC) and export buyers (India GCC)

- "Offer Your Supply" — foreign exporters (Vietnam, Malaysia, Egypt)

Trust strip: COA per lot  ·  Whiteness & particle size tested  ·  MSDS available  ·  Sample in 3–5 days

## Section 2 — The dual business model — export and import

India both exports calcite/GCC and imports specialty grades — we operate on both sides.

Export side — India GCC:

India is a significant exporter of ground calcium carbonate (GCC) — 4,880 export shipments in 2023–24, growing at 23% annually. India's Rajasthan and Gujarat deposits produce high-purity calcite (CaCO₃ 97–99%) with good whiteness — competitive for paints, rubber, paper and construction filler applications in Nepal, Bangladesh, Russia and Africa. Export is completely free — no restrictions, no licensing.

Import side — Specialty coated GCC and PCC:

India imports 10,495 shipments of calcium carbonate annually — primarily coated GCC and PCC from Vietnam, Malaysia and Egypt. Why? Indian domestic deposits lack the whiteness (GE 95+), ultra-fine particle size (D50 1–3 µm) and consistent stearic acid coating quality required by Indian PVC pipe manufacturers, rigid PVC compounders and specialty plastics producers. The PVC and plastics industry specifically demands imported grades because domestic calcite at equivalent particle size and coating quality is not available at competitive cost. We import and supply these grades to Indian industry.

## Section 3 — Understanding the grades: GCC vs PCC vs Coated

GCC — Ground Calcium Carbonate

Produced by mechanical grinding and air classification of natural calcite or limestone — no chemical change. Final product purity and whiteness depends entirely on ore quality. India's Rajasthan calcite produces GCC with CaCO₃ 97–99% and whiteness 88–94 GE — good for paints, rubber and paper at coarser grades. For ultra-fine (D50 below 5 µm) with whiteness above 95 GE, Vietnam and Malaysia origin is superior.

Coated GCC — Stearic acid surface treated

When GCC powder is surface-treated with stearic acid or zinc stearate, the hydrophilic surface becomes hydrophobic — this dramatically improves compatibility with polymer matrices (PVC, PP, HDPE). Coated GCC disperses better in plastic compounds, improves processing, and reduces oil absorption. The PVC pipe industry specifically requires coated GCC — uncoated grade causes processing problems. India imports large volumes of coated GCC from Vietnam and Malaysia.

PCC — Precipitated Calcium Carbonate

Produced by chemical synthesis — burning limestone to lime (CaO), slaking to calcium hydroxide, then reacting with CO₂. The crystal morphology (scalenohedral, rhombohedral, aragonite) and particle size are precisely controlled during precipitation — this is impossible with GCC. PCC achieves D50 as low as 0.07 µm (nano-PCC) with very high whiteness (98+ GE) and low oil absorption after coating. Used in premium PVC, flexible PVC, specialty paper and pharmaceutical applications. India is the world's second-largest PCC importer.

## Section 4A — Export grades: GCC from India — full specifications

| Parameter | Coarse GCC (100–200 mesh) | Fine GCC (325–500 mesh) | Micronised GCC (800–1500 mesh) | Coated GCC (stearic acid) |
| --- | --- | --- | --- | --- |
| CaCO₃ % min | 97.0% | 98.0% | 98.5% | 98.0% |
| Whiteness (GE) | 88–92 | 90–94 | 92–96 | 92–96 |
| Brightness | 86–90 | 88–92 | 90–95 | 90–95 |
| Moisture % max | 0.5% | 0.3% | 0.3% | 0.3% |
| Fe₂O₃ % max | 0.10% | 0.08% | 0.05% | 0.05% |
| MgO % max | 1.0% | 0.8% | 0.5% | 0.5% |
| LOI % (at 900°C) | 42–44% | 42–44% | 42–44% | 42–44% |
| D50 particle size | 15–30 µm | 5–10 µm | 1.5–3 µm | 2–5 µm |
| D97 particle size | 60–100 µm | 20–40 µm | 8–15 µm | 10–20 µm |
| Bulk density | 0.8–1.0 g/cc | 0.7–0.9 g/cc | 0.5–0.7 g/cc | 0.5–0.7 g/cc |
| Surface treatment | None | None | None | Stearic acid coated |
| Oil absorption | 18–22 g/100g | 20–25 g/100g | 22–28 g/100g | Low — 12–18 g/100g |
| Origin | Rajasthan / Gujarat | Rajasthan / Gujarat | Rajasthan | Rajasthan |
| Primary use | Paints, construction, paper filler | Paints, rubber, PVC, paper | Plastics, premium coatings | PVC, rubber, plastics — hydrophobic surface |

Export destinations: Nepal (47% of India's exports) · Bangladesh · Russia · Kenya · UAE · Bhutan

- India's Rajasthan calcite belt (Udaipur, Alwar, Jodhpur) produces the highest quality domestic GCC — 500+ processors active

- Coated grade (stearic acid) available from Rajasthan processors — suitable for rubber and standard plastic applications

- All grades: COA per lot with CaCO₃%, whiteness, brightness, D50, D97, moisture, oil absorption

## Section 4B — Import grades: Coated GCC & PCC from Vietnam / Malaysia / Egypt — full specifications

| Parameter | Coated GCC (imported) | PCC — Scalenohedral | PCC — Rhombohedral | ACC (Activated PCC) |
| --- | --- | --- | --- | --- |
| CaCO₃ % min | 98.5% | 98.0% | 98.5% | 97.0% |
| Whiteness (GE) | 95–98 | 96–99 | 95–98 | 94–97 |
| D50 particle size | 1–5 µm | 0.5–2 µm | 1–3 µm | 0.05–0.1 µm (nano) |
| Moisture % max | 0.3% | 0.3% | 0.3% | 0.5% |
| Bulk density | 0.4–0.7 g/cc | 0.3–0.5 g/cc | 0.5–0.7 g/cc | 0.2–0.4 g/cc |
| Surface treatment | Stearic acid coated | Stearic acid coated | None / coated | Activated |
| Oil absorption | 8–14 g/100g | 10–16 g/100g | 15–20 g/100g | Very low |
| pH (10% suspension) | 8.5–9.5 | 8.5–9.5 | 9.0–9.5 | 8.5–9.5 |
| Origin | Vietnam / Malaysia / Egypt | Vietnam / Malaysia | Vietnam / Egypt | Vietnam / Malaysia |
| Primary use | PVC pipes, rigid PVC, plastics | Flexible PVC, paper, sealants | Paints, rubber | Premium PVC, specialty plastics |

Why Indian industry imports:

- PVC pipe manufacturers: require coated GCC with D50 1–3 µm, whiteness ≥95 GE, stearic acid coating ≥1% — Indian domestic grades cannot consistently match this at competitive price

- Rigid PVC compounders: need nano-PCC (D50 0.05–0.1 µm) for impact modifier effect — not produced domestically at scale

- Flexible PVC (cables, flooring): scalenohedral PCC for reinforcement and processing improvement

- Paper coating: ultra-high brightness (GE 97+) PCC slurry — Indian GCC too coarse and low brightness for paper coating

- Top Indian importers of CaCO₃: Omya India (32%), Rathi Polychem, speciality plastics compounders across Gujarat, Maharashtra, Tamil Nadu

## Section 5 — Applications by industry

PVC pipes & fittings (largest Indian buyer segment for imported grades)

Calcium carbonate is added at 5–25 phr in rigid PVC pipes — reduces cost, improves stiffness, and aids processing. However it must be ultra-fine coated GCC or PCC: uncoated or coarse grades cause fish-eyes, surface defects and reduced impact strength. Indian pipe manufacturers (Supreme, Astral, Finolex supply chain) import coated GCC from Vietnam and Malaysia specifically because domestic grades do not meet the D50 and coating quality requirement.

Paints & coatings (India GCC export grade)

GCC used as a functional extender in interior and exterior emulsion paints — improves opacity, reduces TiO₂ usage, controls sheen and improves scrub resistance. For exterior paints, coarser GCC (D50 10–20 µm) is standard; for smooth interior finishes, finer grades (D50 3–8 µm) are used. Indian GCC (Rajasthan origin) is competitive for paint filler applications in Nepal, Bangladesh and Gulf.

Rubber & sealants

GCC as reinforcing filler in rubber — improves tensile strength, hardness and abrasion resistance at lower cost than silica. Coated grades essential for good dispersion. India exports uncoated and coated GCC for rubber applications; also imports finer PCC grades for premium rubber applications.

Paper manufacturing

PCC used as paper filler and coating pigment — improves brightness, smoothness and printability. Ultra-high whiteness (GE 97+) PCC in slurry form is the standard for coated paper and board. India imports PCC for paper applications from Vietnam and Malaysia.

Pharmaceuticals & food

Food-grade and pharma-grade PCC used as calcium supplement, antacid, excipient and stabiliser. Requires strict heavy metals limits and pharmacopoeia compliance (IP/BP/USP). India imports these specialty grades from certified manufacturers.

## Section 6 — Why buy from us

| Quality & consistency - Fixed mine source (Rajasthan/Gujarat) for export grades — consistent CaCO₃ and whiteness - Fixed origin (Vietnam/Malaysia) for imported grades — consistent particle size lot to lot - Full COA per lot: CaCO₃%, whiteness, brightness, D50, D97, moisture, oil absorption - SGS / Intertek inspection available on request - MSDS and packing list with every consignment | Supply & commercial - Both export (India GCC) and import (coated/PCC) grades from one supplier - MOQ 1 MT for trial orders - Ex-stock at JNPT / Mundra for standard imported grades - Competitive pricing for both domestic supply and export - Sample dispatched within 3–5 days |
| --- | --- |

## Section 7

Foreign Suppliers Welcome

India is one of the world's largest importers of calcium carbonate — 10,495 shipments annually and growing at 34%. Vietnam, Malaysia and Egypt currently dominate supply, and with India's PVC, plastics and paints industries expanding rapidly, this demand is only going to grow. If you produce coated GCC, PCC or specialty calcium carbonate grades and are exploring the Indian market, we are a buyer worth knowing.

We are looking for suppliers who can work with us on credit-based payment terms (DA / Net 45- 60 days) — if this matches how you work with established buyers, we would be glad to hear from you.

What we look for in a supplier:

- Coated GCC: CaCO₃ ≥98% · Whiteness ≥95 GE · D50 1–5 µm · Stearic acid coating ≥1% · COA per lot

- PCC scalenohedral: CaCO₃ ≥98% · Whiteness ≥96 GE · D50 0.5–2 µm · COA per lot

- Origin: Vietnam, Malaysia, Egypt preferred

To start a conversation: Company · Country · Product (coated GCC / PCC / uncoated GCC) · D50 · Whiteness GE · Monthly capacity (MT) · FOB price · Payment terms · Contac

## Section 8 — Mine owners & processors (for India GCC export)

We source GCC from Rajasthan (Udaipur, Alwar, Jodhpur) and Gujarat processors for export to Nepal, Bangladesh and other markets. If you have a calcite grinding unit with consistent quality and monthly output, we want to hear from you.

What we need: CaCO₃ ≥97% · Whiteness ≥88 GE · Consistent mesh size · Monthly capacity ≥50 MT · Contact number

## Section 9 — Logistics

Export (India GCC to Nepal/Bangladesh/international):

- Packaging: 25kg / 50kg PP bags · 1MT jumbo bags

- Ports: Mundra / Kandla (Rajasthan origin) · Kolkata (for Nepal/Bangladesh road/rail)

- Transit: Bangladesh 5–8 days · Nepal road · Russia 20–28 days

- HS Code: 2836.50 (calcium carbonate) · 2517.20 (marble granules/powder) depending on grade

Import (Coated GCC / PCC from Vietnam/Malaysia for Indian industry):

- Packaging: 25kg bags in 1MT jumbo bags (standard for PCC) · 50kg bags for coated GCC

- Entry ports: JNPT / Nhava Sheva (primary) · Mundra · Chennai

- Transit: Vietnam/Malaysia 10–15 days · Egypt 18–24 days

- Lead time: ex-stock 3–7 days · fresh import 25–35 days

Frequently Asked Questions

### Why does India import calcium carbonate?

India produces standard GCC, but ultrafine coated grades (high whiteness, low D50) are imported for PVC and premium applications.

### Q2. What is the difference between GCC and PCC?

- GCC → natural, milled, cost-effective

- PCC → synthetic, ultra-fine, better performance but higher cost

### Q3. Why is coated GCC required for PVC?

Coating improves dispersion and bonding in PVC.
Uncoated GCC can cause defects and is used only in low-grade applications.

### Q4. What specs are needed for paint applications?

- Standard paints → whiteness 88–92 GE, D50 10–20 µm

- Premium paints → higher whiteness and finer particle size

### Q5. Can Indian GCC be exported?

Yes, for standard applications.
Premium PVC grades typically require imported coated GCC.

### Q6. What is MOQ and sample time?

- MOQ: 1 MT

- Samples with COA: 3–5 days

### Q7. What are the payment terms?

We work on Advance and LC (Letter of Credit) terms.