CALCIUM ALUMINATE CEMENT (CAC)

High-Alumina Refractory Binder  ·  CAC 40 · CAC 50 · CAC 70 · CAC 80  ·  Imported & Supplied to Indian Steel, Petrochemical & Infrastructure Industry

## Section 1 — Hero content

Calcium Aluminate Cement — CAC 40 · CAC 50 · CAC 70 · CAC 80 — Imported & Supplied to Indian Refractory, Steel & Infrastructure Industry

Sub-headline: Al₂O₃ 40–80%  ·  Rapid strength gain (80% in 6–24 hrs)  ·  Thermal resistance to 1,700°C  ·  Sulphate & chemical corrosion resistant  ·  Imported from China, Turkey, France  ·  CIF Indian ports

Single CTA: "Request a Quote / Sample COA"

Trust strip: ISO 9001  ·  COA per lot  ·  ASTM C1157 / EN 14647 compliant  ·  Sample in 3–5 days  ·  25kg bags & bulk supply

## Section 2 — What is Calcium Aluminate Cement?

Calcium Aluminate Cement (CAC) — also called high alumina cement or aluminous cement — is a specialty hydraulic binder produced by fusing or sintering bauxite and limestone at high temperature. The primary mineral phases are calcium monoaluminate (CaO·Al₂O₃) and calcium dialuminate (CaO·2Al₂O₃) — these give CAC its defining properties that ordinary Portland cement cannot match.

CAC is not a construction cement in the conventional sense. It is a precision industrial binder used where three specific performance requirements exist simultaneously — high-temperature resistance up to 1,700°C, rapid strength development and chemical corrosion resistance.

The global CAC market was valued at USD 4.5 billion in 2024 and is projected to reach USD 7.5 billion by 2033 at a CAGR of 5.7% — driven by the steel sector's shift toward electric arc furnaces requiring CAC-based monolithic refractories. In India, where EAF adoption grew by 18% in 2023–24, CAC demand for refractory castables surged 22%.

## Section 3 — The key difference from ordinary cement

Most buyers encounter CAC for the first time when ordinary Portland cement fails in their application. The table below explains why:

| Property | Ordinary Portland Cement | Calcium Aluminate Cement |
| --- | --- | --- |
| Max service temp | 300°C (degrades above) | 1,300–1,700°C (grade dependent) |
| Time to 80% strength | 28 days | 6–24 hours |
| Sulphate resistance | Poor — primary failure mode | Excellent |
| Chemical resistance | Moderate | High — acids, alkalis, H₂S |
| Alumina (Al₂O₃) content | 5–8% | 40–80% |
| Primary application | General construction | Refractories, rapid repair, chemical environments |
| Relative cost | Low | 5–15x higher than OPC |

The alumina content is the defining parameter — higher Al₂O₃ = higher service temperature, better chemical resistance, better hot strength. Grade selection (CAC 40/50/70/80) is always a function of your maximum service temperature and chemical environment.

## Section 4 — Full grade specifications (compact)

| Parameter | CAC 40 | CAC 50 | CAC 70 | CAC 80 |
| --- | --- | --- | --- | --- |
| Al₂O₃ % min | 38–42% | 48–52% | 68–72% | 78–82% |
| CaO % | 35–40% | 28–35% | 18–25% | 12–18% |
| SiO₂ % max | 5.0% | 4.0% | 1.0% | 0.5% |
| Fe₂O₃ % max | 3.0% | 2.5% | 0.3% | 0.3% |
| Initial setting time | 2–4 hours | 2–5 hours | 3–6 hours | 3–8 hours |
| 24h compressive strength | ≥40 MPa | ≥50 MPa | ≥60 MPa | ≥60 MPa |
| Max service temp | 1,350°C | 1,450°C | 1,600°C | 1,700°C |
| Colour | Grey/brown | Grey | White/cream | White |
| Standard | ASTM C1157 · EN 14647 | ASTM C1157 · EN 14647 | EN 14647 | EN 14647 |
| Origin | China | China / Turkey | China / Turkey / France | France / China |
| Primary use | Refractory castables, rapid repair, wastewater | Monolithic refractories, ladles, tundishes | High-temp refractories, EAF linings | Ultra-high temp, kiln furniture |

Additional notes:

- CAC 40 suits rapid repair, self-leveling floors, non-shrink grouts and low-duty refractory castables — most cost-effective grade

- CAC 70 is the dominant market grade — high alumina, low iron (Fe₂O₃ ≤0.3%), suitable for white/cream colour-sensitive applications

- Low cement castables (LCC) use CAC at 3–8% addition — better hot strength, lower porosity than conventional castables using 15–25% CAC

- COA per lot: Al₂O₃%, CaO%, SiO₂%, Fe₂O₃%, initial & final setting time, 24-hour and 28-day compressive strength

- Storage critical: sealed moisture-proof bags only — even brief humidity exposure causes premature hydration. Shelf life 6 months from manufacture

## Section 5 — Applications in India

Refractory castables for steel industry (largest segment)

Refractories absorbed 55% of global CAC volume in 2024 — Indian EAF steel plants (Raipur, Vizag, Kutch clusters) are primary buyers of CAC 50, 60 and 70 for ladle and tundish linings, tap hole repair and emergency furnace patching. CAC consumption in Indian steel refractories grew 22% in 2023–24 driven by EAF adoption — a structural, multi-year demand driver.

Refractory castable manufacturers

India has 200+ refractory castable manufacturers supplying steel, cement, glass and non-ferrous industries. These manufacturers buy CAC as a binder — blended with calcined alumina, fused alumina and other aggregates — to produce their branded castable products. This is a large, consistent domestic buyer segment purchasing monthly.

Petrochemical and chemical plants

The chemical sector accounted for 22% of global CAC demand in 2024, driven by ethylene cracker furnace linings, reactor vessels and process equipment linings where aggressive chemical environments destroy ordinary refractory materials rapidly. Indian refineries and petrochemical complexes in Gujarat, Maharashtra and Odisha are active buyers.

Wastewater infrastructure

CAC 40-based mortars resist hydrogen sulphide-induced biogenic sulphuric acid corrosion in sewage pipelines and tunnels — H₂S generated by bacteria in sewage attacks ordinary concrete aggressively. CAC-modified concrete extends pipe and tunnel service life from 10–15 years to 50+ years. India's urban sewage expansion under Smart Cities Mission and AMRUT schemes is driving growing CAC demand in this segment.

Rapid repair and construction

CAC's ability to reach 80% final strength in 6 hours makes it ideal for road and runway repairs, bridge deck patching, industrial floor restoration — wherever extended curing closure causes significant operational loss. Airport runway repairs and expressway maintenance contractors are active buyers.

Cement kilns, glass furnaces and non-ferrous smelting

CAC castables used in transition zones and burning zones of cement kilns, glass tank linings, and aluminium/copper/zinc smelter linings — where extreme temperatures and aggressive chemical slags destroy standard refractories within weeks.

## Section 6 — India market context & source countries

India does not produce CAC at meaningful commercial scale. CAC 50, 70 and 80 are almost entirely imported. India's CAC imports are growing at 15–20% annually driven by EAF steel expansion, petrochemical investment and wastewater infrastructure spending.

Source countries:

- China — largest volume, most competitive pricing; primary source for CAC 40 and CAC 50. Major producers: Zhengzhou Kerui, Kaifeng Datong, Henan Haojiaye

- Turkey (Çimsa) — high quality CAC 50 and 70, consistent European-standard documentation; Çimsa invested USD 31.75 million in capacity expansion in 2024

- France (Imerys / Kerneos / Secar) — premium CAC 70 and 80 (SECAR 71 brand widely specified); preferred by EPC contractors requiring European documentation for international projects

## Section 7 — Why buy from us

| Quality & consistency - All four grades (CAC 40/50/70/80) from one supplier - Full COA per lot: Al₂O₃%, CaO%, SiO₂%, Fe₂O₃%, setting time, compressive strength - SGS / Intertek inspection at origin available - MSDS and technical data sheet per grade | Supply & commercial - MOQ 2 MT for trial orders — no large commitment - Ex-stock at JNPT / Mundra for CAC 40 and CAC 50 standard grades - Competitive CIF / DAP pricing to your plant - Sample with COA dispatched within 3–5 days - Lead time: ex-stock 3–7 days · fresh import 25–35 days |
| --- | --- |

## Section 8 — Foreign Suppliers Welcome

India's growing steel, refractory and infrastructure sectors are creating consistent and expanding demand for CAC — particularly CAC 50, 70 and 80 which are almost entirely imported. If you are a CAC manufacturer or export trading company looking for a reliable Indian buyer, we are worth talking to.

We value supplier partnerships built on mutual trust and commercial flexibility. If you are open to structured, credit-based arrangements that allow both sides to build confidence over time, we would genuinely like to hear from you.

What we look for:

- CAC 40: Al₂O₃ ≥38%  ·  Setting time within EN 14647 limits  ·  COA per lot  ·  Origin: China

- CAC 50: Al₂O₃ ≥48%  ·  24h strength ≥50 MPa  ·  COA per lot  ·  Origin: China / Turkey

- CAC 70: Al₂O₃ ≥68%  ·  Fe₂O₃ ≤0.3%  ·  COA per lot (SGS/BV preferred)  ·  Origin: China / Turkey / France

- CAC 80: Al₂O₃ ≥78%  ·  Fe₂O₃ ≤0.3%  ·  Origin: France / China

To start a conversation: Company · Country · Grade(s) available · Al₂O₃ %  · Monthly capacity (MT) · FOB price · Payment terms · Contact

## Section 9 — Logistics

- Packaging: 25kg multilayer moisture-resistant paper bags (critical — CAC degrades on humidity exposure)  ·  1MT jumbo bags  ·  bulk FCL

- Storage: dry, sealed, covered warehouse  ·  away from floor contact  ·  use within 6 months of manufacture date

- Ports: JNPT / Nhava Sheva (primary)  ·  Mundra  ·  Chennai

- Transit: China 15–20 days  ·  Turkey 18–24 days  ·  France 22–28 days

- HS Code: 2523.90 (other hydraulic cements — calcium aluminate cement)

- Inland delivery: Raipur (steel/refractory cluster)  ·  Vizag  ·  Bhilai  ·  Pune  ·  Ahmedabad  ·  Mumbai

- Lead time: ex-stock CAC 40/50: 3–7 days  ·  CAC 70/80 fresh import: 25–35 days

## Section 10 — Contact + SEO

Buyer form fields:

- Company · State/City · Grade (CAC 40/50/70/80) · Application (refractory castable / steel ladle / wastewater / rapid repair / petrochemical) · Qty/month (MT) · Delivery location

SEO target keywords:

calcium aluminate cement India · high alumina cement supplier India · CAC 70 importer India · refractory cement India · aluminous cement India · calcium aluminate cement for castables · CAC 40 supplier India · high alumina cement refractory India · calcium aluminate cement price India · CAC importer India

Frequently Asked Questions

Q1. What is calcium aluminate cement and how is it different from ordinary Portland cement?

CAC is a specialty hydraulic binder with 40–80% alumina — it withstands temperatures up to 1,700°C and resists sulphate and acid attack that destroys ordinary Portland cement (5–8% alumina, max 300°C). CAC also reaches 80% final strength in 6–24 hours vs 28 days for OPC.

Q2. Which CAC grade should I specify for my EAF steel plant ladle lining?

CAC 50 for general duty ladles and CAC 70 for ladles handling aggressive slags or higher pouring temperatures — specify your maximum service temperature and slag chemistry and we will confirm the appropriate grade and mix design recommendation.

Q3. Can CAC be used to repair sewage pipes and tunnels?

Yes — CAC 40 resists biogenic sulphuric acid (H₂SO₄) generated by H₂S gas in sewage environments, which destroys ordinary concrete rapidly. CAC-modified concrete in sewage infrastructure extends service life from 10–15 years to 50+ years.

Q4. What is the difference between low cement castables (LCC) and conventional castables?

Conventional castables use 15–25% CAC; LCC uses 3–8% CAC with microsilica and dispersants — giving lower porosity, higher density and better hot strength. The CAC grade and addition level must match your specific castable system design.

Q5. What is the minimum order and sample lead time?

MOQ is 2 MT for trial orders; samples with full COA (Al₂O₃%, CaO%, SiO₂%, Fe₂O₃%, setting time, 24-hour strength) dispatched within 3–5 days. Contact us with your grade and application and we confirm stock availability and pricing.

Q6. How should CAC be stored to prevent quality degradation?

Store in dry, sealed, moisture-proof conditions — even brief humidity exposure triggers premature hydration and reduces strength development significantly. Use sealed bags in a covered dry warehouse, no floor contact, and use within 6 months of the manufacture date on the bag.