DOLOMITE — RAW, CALCINED & SINTERED

Agricultural · Glass & Ceramic · Animal Feed · Calcined · Sintered / Dead Burnt  ·  Rajasthan Origin, India

## Section 1 — Hero content

Dolomite — Raw, Calcined & Sintered from India  ·  Agricultural, Glass, Refractory & Industrial Grades  ·

Sub-headline: Raw dolomite · Calcined dolomite (light/dead burnt) · Sintered dolomite  ·  MgO 18–40%  ·  100 to 500 mesh  ·  50kg bags, jumbo bags & clinker bulk  ·  FOB Mundra / Kandla

Single CTA: "Request Quote / Sample"

Trust strip: ·  COA with every lot  ·  Rajasthan origin  ·  Sample in 7 days

- WhatsApp button — Bangladesh ceramic buyers and agricultural dealers prefer WhatsApp

- Do NOT claim to be a major dolomite exporter — position honestly as reliable supply for specific grades

## Section 3 — Product grades — full specifications

Four grades, each targeting a specific buyer vertical. Full chemistry table below:

| Parameter | Agricultural | Industrial / steel flux | Glass & ceramic | Animal feed / pharma | Calcined dolomite | Sintered dolomite |
| --- | --- | --- | --- | --- | --- | --- |
| CaCO₃ / CaO | CaCO₃ 54–58% | CaCO₃ 52–58% | CaCO₃ 52–56% | CaCO₃ 55–60% | CaO 38–42% (free) | CaO 36–40% |
| MgCO₃ / MgO | MgCO₃ 38–42% | MgCO₃ 36–42% | MgCO₃ 38–44% | MgCO₃ 40–44% | MgO 32–38% (free) | MgO 35–40% |
| SiO₂ % max | 3.0% | 2.5% | 1.5% | 1.0% | 2.0% | 1.5% |
| Fe₂O₃ % max | 0.5% | 0.5% | 0.15% | 0.10% | 0.5% | 0.5% |
| Al₂O₃ % max | 1.5% | 1.5% | 0.8% | 0.5% | 1.0% | 1.0% |
| LOI % | 45–48% | 44–48% | 44–48% | 44–48% | <1.0% (CO₂ driven off) | <0.5% |
| Moisture % max | 1.0% | 1.0% | 0.5% | 0.3% | 0.5% | 0.3% |
| Calcination temp | — | — | — | — | 800–900°C | 1450–1550°C |
| Whiteness (GE) | 80–86 | 75–84 | 86–92 | 88–94 | 85–90 | Colour not critical |
| Bulk density | — | — | — | — | 0.7–0.9 g/cc | 2.8–3.0 g/cc |
| Form / size | 100/200 mesh · 1–5mm granules · lumps | 0–50mm lumps · 6–25mm crushed | 200/300/400 mesh · D50 15–30µm | 200/300/500 mesh food-grade | 200 mesh powder · 1–5mm granules | 1–25mm clinker / aggregate |
| Heavy metals | — | — | Low Fe critical | Pb, As, Cd, Hg limits | — | — |
| Primary use | Soil pH, Ca+Mg fertiliser | Flux in BOF/EAF | Glass batch, ceramic glaze | Poultry/cattle feed, antacid | Steel flux, refractories, water treatment, soil amendment | High-temp refractories, EAF/BOF lining, kiln furniture |

Six grades covered — raw through to fully sintered:

- Raw dolomite: agricultural, industrial flux, glass/ceramic, animal feed — 4 grades differentiated by purity and mesh

- Calcined dolomite: fired at 800–900°C; CO₂ driven off; reactive CaO+MgO powder or granules; MgO 32–38% (free)

- Sintered / dead burnt dolomite: fired at 1450–1550°C; dense inert clinker; MgO 35–40%; used in high-temp refractories

- All grades: COA per lot — CaO, MgO, SiO₂, Fe₂O₃, Al₂O₃, LOI, moisture, whiteness

- Downloadable typical COA as PDF available for each grade on request

- Custom mesh size available for orders of 2 MT and above

## Section 4 — Applications — who uses dolomite and why

- Agriculture (largest domestic market): dolomite powder corrects soil pH in acidic soils — neutralises excess H⁺ ions; simultaneously supplies calcium and magnesium micronutrients that single-nutrient lime cannot; ground to 100–200 mesh for field application; used under India's Soil Health Card Scheme; buyers are agri input dealers, fertiliser distributors, cooperatives

- Glass manufacturing: dolomite is an essential MgO and CaO source in float glass, container glass and specialty glass batch — improves durability, reduces thermal expansion, lowers melting temperature; low Fe₂O₃ (below 0.15%) critical to avoid colouration; Bangladesh float glass industry is an active buyer of Indian dolomite

- Ceramics & tiles: flux in ceramic body and glaze — lowers firing temperature, improves surface finish; used in wall tile bodies, ceramic frits; Bangladesh and Southeast Asian tile manufacturers are buyers

- Animal feed: dolomite provides Ca and Mg in broiler, layer and cattle feed — more balanced than pure limestone; must meet food-grade heavy metal limits; large domestic poultry belt (AP, Telangana, Maharashtra) is the buyer base

- Paints & coatings: functional extender and filler — improves hiding power, reduces cost, provides mild alkali character; fine ground grades (300–500 mesh) used in exterior emulsions and putty

- Rubber & plastics: inert filler improving hardness and reducing compound cost; stearic acid coated grade available

- Calcined dolomite (light burnt, 800–900°C): CO₂ is driven off producing a reactive CaO+MgO powder — used as steel flux in BOF and EAF furnaces (reacts faster than raw dolomite), soil amendment (higher reactivity than raw for quick pH correction), water treatment (neutralises acidic effluent), and refractory binder; available as fine powder (200 mesh) and granules (1–5mm)

- Dead burnt / sintered dolomite (1450–1550°C): fired at very high temperature to produce dense, inert CaO+MgO clinker with very low reactivity — used for high-temperature refractory bricks and ramming mass in EAF/BOF steel furnace linings, ladle linings, cement kiln refractories, and glass furnace applications; bulk density 2.8–3.0 g/cc; supplied as 1–25mm clinker or crushed aggregate

- Construction: aggregate and concrete filler — low-margin, high-volume domestic application; not an export target

## Section 5 — Why buy from us — buyer advantages

| Quality & consistency - Fixed Rajasthan source — same quarry, same chemistry lot to lot - In-house XRF and whiteness testing — every lot checked before dispatch - COA with every shipment — no chasing for documents - Grade-specific mesh screening — no off-spec particle size in your bag - Sample with full COA dispatched in 7 days — fast qualification | Supply & logistics - Multiple grades from one supplier — simplify your procurement - Flexible quantity — 500kg trial to full container lots - FOB Mundra / Kandla for export · road delivery pan-India - LCL available from 500kg — no need to fill a container for trials - Payment Term – TT , LC |
| --- | --- |

## Section 6 — Partner with us — quarry & mine owners

For Rajasthan dolomite quarry owners and crusher operators:

- We buy dolomite lumps, crushed and ground grades from Rajasthan quarries — Ajmer, Udaipur, Beawar and surrounding areas

- What we need: MgO 18%+, SiO₂ below 3%, consistent supply of minimum 50 MT/month

- What we offer: regular monthly offtake, grade-linked pricing (higher purity = better rate), payment on committed timelines, no arbitrary deductions

- We handle all processing, documentation and export logistics — zero burden on you

Supplier enquiry form fields:

- Name · District/Quarry location · Grade (lumps/crushed/ground) · MgO % (approx) · Monthly output (MT) · Contact number

## Section 7 — Origin — Rajasthan dolomite belt

- Rajasthan accounts for over 50% of India's total dolomite production — the Ajmer, Udaipur and Beawar districts host the highest-quality deposits with naturally high MgO and bright white colour

- Indian dolomite geology: formed in Precambrian marine sedimentary environments — produces highly crystalline, low-iron material ideal for glass and ceramic applications where whiteness is critical

- Processing chain: open quarry → jaw crushing → rod/ball mill grinding → air classification → screening → packaging; calcination available for refractory grades

- Proximity to Mundra and Kandla ports (6–8 hours from Rajasthan) — freight advantage for export to Bangladesh and Southeast Asia

# FREQUENTLY ASKED QUESTIONS (SHORT VERSION)

### Q1. What is the difference between dolomite and limestone?

Dolomite contains both calcium and magnesium (CaMg(CO₃)₂), while limestone is mainly calcium carbonate.
Dolomite is preferred where magnesium is also required, such as agriculture, glass, and feed applications.

### Q2. Which dolomite grade is suitable for agriculture?

Agricultural dolomite typically has:

- MgO: 18–21%

- Mesh: 100–200

Granular sizes (1–5 mm) are also available for easy field application.

### Q3. What Fe₂O₃ level is required for glass-grade dolomite?

For glass manufacturing:

- Fe₂O₃: below 0.10–0.15%

Low iron ensures clear glass without color tint.

### Q4. What is the minimum order and sample availability?

- Samples: available for testing

- Bulk orders: typically 1 MT or container basis

Trial orders can be arranged before regular supply.

### Q5. Can dolomite be used in animal feed?

Yes, dolomite is used in feed as a calcium and magnesium source, provided it meets low heavy metal limits and quality standards.

### Q6. What is the difference between calcined and sintered dolomite?

- Calcined dolomite → reactive, used in steel flux, soil, water treatment

- Sintered (dead burnt) → dense, high-temperature resistant, used in refractories

### Q7. What are the payment terms?

We work with:

- TT (advance / partial advance)

- LC at sight

.

### Q8. Why should buyers source dolomite from us?

- Consistent quality across shipments

- Multiple sourcing options across India

- Competitive pricing

- Flexible specifications and sizing

- Reliable supply and quick response