WHITE & BROWN FUSED ALUMINA

Imported from China & Global Sources  ·  Reliable Supply for Indian Abrasive, Refractory & Blasting Industry

WFA (White) Al₂O₃ ≥99.5%  ·  BFA (Brown) Al₂O₃ ≥95%  ·  All FEPA Grit Sizes  ·  Refractory Aggregates  ·  Micro-Powder

## Section 1 — Hero content

White & Brown Fused Alumina — Imported from China & Global Sources — Reliable Supply for Indian Abrasive, Refractory & Blasting Industry

Sub-headline: WFA Al₂O₃ ≥99.5% · BFA Al₂O₃ ≥95% · FEPA F-grit & P-grit · Refractory sizes 0–8mm · Micro-powder available · CIF Indian ports

Two CTAs:

- "Enquire for Supply / Get a Quote" — for Indian buyers

- "Offer Your Fused Alumina Supply" — for Chinese and global exporters

Trust strip: · COA with every lot · · Ex-stock at JNPT/Mundra

- WhatsApp + phone — Indian abrasive plant buyers prefer WhatsApp; Chinese exporters also use WhatsApp

## Section 2 — Trust bar (5 stats)

- MT imported and supplied per year to Indian industry

- Indian industries supplied: abrasive manufacturers · refractory producers · blasting contractors · grinding wheel makers

- Source countries: China (primary, 99% of India's imports) · Malaysia · Japan — multiple origins for supply security

- Grades: WFA (white) + BFA (brown) — all FEPA grit sizes F4–F220 and refractory sizes 0–8mm in stock

- Lead time: ex-stock at Indian port 3–7 days · fresh import 30–40 days from order

## Section 3 — White Fused Alumina (WFA) — full specifications

Production: fusing high-purity Bayer process alumina in an electric arc furnace at over 2000°C, followed by slow solidification, crushing, magnetic separation, and precision sieving. Result: α-Al₂O₃ corundum, white colour, ultra-high purity, highly friable.

| Parameter | Standard WFA (abrasive) | High-purity WFA (refractory) | Micro-powder WFA |
| --- | --- | --- | --- |
| Al₂O₃ % min | ≥99.0% | ≥99.5% | ≥99.5% |
| SiO₂ % max | 0.10% | 0.06% | 0.05% |
| Fe₂O₃ % max | 0.08% | 0.06% | 0.05% |
| Na₂O % max | 0.40% | 0.30% | 0.25% |
| CaO % max | 0.05% | 0.02% | 0.02% |
| MgO % max | 0.05% | 0.02% | 0.02% |
| TiO₂ % max | 0.03% | 0.02% | 0.02% |
| Mohs hardness | 9 | 9 | 9 |
| Specific gravity | 3.95 g/cc | 3.95 g/cc | 3.95 g/cc |
| Bulk density | 1.75–1.95 g/cc | 1.80–2.00 g/cc | — |
| Melting point | 2050°C | 2050°C | 2050°C |
| Crystal structure | α-Al₂O₃ corundum | α-Al₂O₃ corundum | α-Al₂O₃ corundum |
| Colour | White | White | White powder |
| Grain shape | Sharp blocky (F-grit) / Angular needle (P-grit) | Blocky aggregates | Submicron to 45µm |
| Available sizes | FEPA F12–F220 (macro) · P12–P1200 (micro) | 0–1mm · 1–3mm · 3–5mm · 5–8mm | F280–F1200 · D50 1–45µm |
| Standards | FEPA · ANSI B74.12 · JIS R 6001 | FEPA · ISO 9136 | FEPA F/P micro-grit |
| Primary use | Vitrified/resin grinding wheels · coated abrasives · blasting stainless/non-ferrous | High-alumina refractories · castables · kiln furniture | Polishing · lapping · semiconductor · optical glass |

Key performance advantages:

- Zero iron contamination — mandatory for stainless steel, titanium, aluminium, copper and non-ferrous metal grinding and blasting

- Highly friable (self-sharpening) — grain fractures under load to expose fresh cutting edges; produces cool cutting action preventing workpiece burn

- Na₂O content critical for refractory grade — low Na₂O prevents glassy phase formation at high temperatures, maintaining refractoriness

- COA per lot: Al₂O₃, SiO₂, Fe₂O₃, Na₂O, CaO, MgO, TiO₂, bulk density + FEPA sieve distribution

## Section 4 — Brown Fused Alumina (BFA) — full specifications

Production: fusing calcined bauxite with anthracite (carbon) and iron scrap in an electric arc furnace at ~2000–2200°C. TiO₂ from bauxite remains in finished grain as a toughening agent — this is what gives BFA its characteristic brown colour and impact resistance.

| Parameter | Regular BFA (95%) | High-purity BFA (97%) | Low-iron BFA | Refractory BFA |
| --- | --- | --- | --- | --- |
| Al₂O₃ % min | 95.0% | 97.0% | 95.0% | 95.0% |
| TiO₂ % | 2.0–3.8% | 1.5–2.5% | 1.5–2.5% | 2.0–3.5% |
| SiO₂ % max | 1.5% | 1.0% | 1.2% | 1.5% |
| Fe₂O₃ % max | 0.30% | 0.20% | 0.10% | 0.30% |
| CaO % max | 0.50% | 0.40% | 0.40% | 0.50% |
| Magnetic material % max | 0.05% | 0.03% | 0.03% | 0.05% |
| Mohs hardness | 9 | 9 | 9 | 9 |
| Specific gravity | 3.90–4.10 g/cc | 3.95 g/cc | 3.90 g/cc | 3.90–4.10 g/cc |
| Bulk density | 1.75–1.95 g/cc | 1.80–1.95 g/cc | 1.75–1.90 g/cc | 1.80–2.00 g/cc |
| Micro-hardness | 2000–2200 kg/mm² | 2000–2200 kg/mm² | 2000–2200 kg/mm² | 2000–2200 kg/mm² |
| Melting point | 1950°C | 1950°C | 1950°C | 1950°C |
| Colour | Brown / dark brown | Brown | Brown | Brown |
| Grain shape | Angular, blocky | Angular, blocky | Angular | Blocky aggregates |
| Available sizes | FEPA F4–F220 (macro) · P12–P220 (micro) | F12–F150 | F16–F120 | 0–1 · 1–3 · 3–5 · 5–8mm |
| Standards | FEPA · ANSI B74.4 · ISO 8486 · JIS R 6001 | FEPA | FEPA | ISO 9136 |
| Primary use | General grinding wheels · blasting · sandpaper · standard refractory | Vitrified wheels for steel · precision grinding | Non-ferrous blasting · Al/Cu surface prep | Castables · refractory bricks · BOF lining |

Key performance advantages:

- TiO₂ = toughness agent: higher TiO₂ (2.5–3.8%) → tougher grain → heavy-duty grinding wheels for steel; lower TiO₂ (1.5–2.0%) → sharper grain → coated abrasives (sandpaper, belts)

- Tough, blocky grain resists fracture under high feed rates — longer grinding wheel life on carbon steel vs WFA

- Cost-effective vs WFA for general-purpose steel grinding where iron contamination is not a quality concern

- Magnetic material must be below 0.05% — excess free iron causes grinding wheel imbalance and workpiece contamination

- COA per lot: Al₂O₃, TiO₂, SiO₂, Fe₂O₃, CaO, magnetic material, bulk density + FEPA sieve distribution

## Section 5 — WFA vs BFA — which grade do you need?

Plain-language selection guide for Indian buyers:

- Grinding stainless steel, titanium, aluminium, copper or non-ferrous metals? → WFA only — iron from BFA contaminates the work surface and causes corrosion

- Grinding high-speed steel, alloy steel, hardened tool steel? → WFA preferred — self-sharpening, cool cutting, prevents workpiece burn

- General-purpose grinding of carbon steel, cast iron, low-alloy steel? → BFA (regular grade) — more cost-effective, tough grain survives heavy feed rates

- Blasting carbon or structural steel for rust removal / surface preparation? → BFA F16–F46 standard; low-iron BFA for aluminium / copper profiles

- Making vitrified grinding wheels for precision applications? → WFA (friable, cool cutting) or high-purity BFA (tougher, for carbon steel)

- High-temperature refractories (above 1600°C), castables, kiln furniture? → WFA refractory grade (higher purity, better slag resistance)

- Polishing, lapping, semiconductor or optical glass? → WFA micro-powder F280–F1200

- Not sure? Share your material, application and surface finish requirement — we confirm the right grade and grit size

## Section 6 — Industry applications in India

- Abrasive grinding wheel manufacturers (largest buyer segment): vitrified and resin-bonded wheels — Rajkot cluster has 200+ grinding wheel units; Pune, Chennai, Coimbatore are other major hubs; WFA for stainless/precision, BFA for carbon steel/general-purpose — all FEPA grit sizes

- Coated abrasives (sandpaper, abrasive belts, flap discs): BFA P-grit for paper and cloth backings — high-volume consumption by automotive body shops, furniture industry and sheet metal fabrication

- Refractory manufacturers: castables, monolithic refractories and bricks for steel plants, cement kilns and glass furnaces — WFA aggregate for high-alumina premium castables; BFA for standard-duty refractory applications

- Surface blasting / shot blasting: BFA F16–F46 for structural steel, bridges, ship hulls, pipeline coating preparation; low-iron BFA for aluminium profiles, die castings, aerospace precision components

- Precision investment casting / lost-wax casting: WFA as shell material — high dimensional accuracy, smooth surface, thermal stability; automotive and aerospace foundries in Rajkot, Pune and Coimbatore

- Lapping and polishing: WFA micro-powder (F280–F1200) for optical glass, watch crystals, semiconductor wafers, hard disk substrates

- Anti-skid coatings and industrial flooring: WFA and BFA coarse grits in epoxy flooring, anti-skid paints for factory floors, ramps, aircraft hangars, sports facilities

- Dental polishing and dermatology: ultra-fine WFA micro-powder in dental polishing pastes, prophylaxis products and dermatological microdermabrasion devices

## Section 7 — Why buy from us — buyer advantages

| Quality & consistency - Fixed plant source — same factory, consistent chemistry lot to lot - Full COA: chemistry + FEPA sieve distribution per lot - Magnetic material verified <0.05% — critical for wheel manufacturers - SGS/Intertek inspection at origin available on request - Reference sample retained per lot | Supply reliability - Both WFA and BFA from one supplier — single point of contact - Multiple FEPA grit sizes in stock at Indian port - Ex-stock delivery 3–7 days for stocked grades - Fresh import 30–40 days for non-stock sizes - Long-term supply contracts available | Technical support - Grade and grit size recommendation for your specific application - Custom narrow sieve distributions on request - Technical data sheets per grade - Trial 100–500 kg before bulk commitment - Abrasive and refractory formulation queries supported | Commercial & logistics - Competitive CIF / DAP pricing — landed cost at your plant - 25kg bags and 1MT jumbo bags available - LCL from 500kg for trial orders - REACH, MSDS, COA documentation standard - Payment on committed timelines |
| --- | --- | --- | --- |

Section 8

- Foreign Supplier / Exporter Partnership

- We work directly with fused alumina manufacturers (not traders) for the Indian market. We source WFA (Al₂O₃ ≥99.0% / ≥99.5%) and BFA (Al₂O₃ ≥95% / ≥97%) across FEPA grit sizes and refractory aggregates.

- Material is evaluated on TiO₂ (BFA), Na₂O (WFA) and sieve consistency, not just Al₂O₃. We engage suppliers who can ensure consistent quality, lot-wise COA, controlled magnetic content (≤0.05%) and reliable monthly supply. Malaysia, Japan and other origins.

- Our model is based on long-term, repeat shipment programs, not spot trading. We prefer partners aligned with stable supply cycles and ongoing volume commitments.

- We follow a dual-sourcing approach and welcome qualified manufacturers from China,

## Section 9 — India's fused alumina market — why imports are essential

- India is the world's largest importer of brown fused alumina — leading globally with 6,061 import shipments in the past 12 months, ahead of Vietnam (1,719) and Indonesia (689)

- India does not produce WFA or BFA domestically at commercial scale — no large electric arc furnace fused alumina plant exists; 99% of India's imports originate from China

- India's abrasive industry is large and growing: the Rajkot cluster alone has 200+ grinding wheel manufacturers; coated abrasives, refractory castables, precision casting and blasting media are all large volume segments

- Supply diversification demand: Indian buyers are actively looking beyond China after COVID supply disruptions — Malaysia and Japan origin gaining attention, creating opportunity for non-China suppliers

- Price reference (2025 indicative): WFA abrasive grade USD 600–1,100/MT FOB China; WFA high-purity refractory USD 900–1,600/MT; BFA regular grade USD 400–700/MT FOB China — specific pricing varies with grit size and quantity

## Section 12 — Dual contact forms + SEO block

Indian buyer form fields:

- Company name · State / City · Grade (WFA / BFA / both) · Application (abrasive / refractory / blasting / polishing / other)

- FEPA grit sizes needed · Quantity per month (MT) · Delivery location · Payment method

Foreign supplier form fields:

- Company · Country · Plant location · WFA or BFA (or both) · Al₂O₃ % · Available grit sizes · Monthly export capacity (MT) · FOB price indication · Contact

Response commitment: "Indian buyer enquiries within 2 hours · Supplier enquiries within 24 hours"

# FREQUENTLY ASKED QUESTIONS

### Q1. What is the difference between white and brown fused alumina?

- WFA → high purity, iron-free, used for precision and stainless applications

- BFA → tougher, cost-effective, used for general grinding and blasting

### Q2. What grit sizes are available?

We supply FEPA F-grits (F16–F120) for abrasives and 0–1mm to 5–8mm sizes for refractories.
Custom sizes can be arranged.

### Q3. Why is TiO₂ important in BFA?

- Higher TiO₂ → stronger, tougher grain

- Lower TiO₂ → sharper cutting

It affects grinding performance.

### Q4. What is the minimum order and lead time?

- Minimum: 500 kg (trial possible)

- Stock material: 3–10 days delivery

- Fresh import: 30–40 days

### Q5. How do import duties affect pricing?

Fused alumina has applicable import duty.
We provide final landed cost including customs before order confirmation.

### Q6. Can WFA and BFA be shipped together?

Yes, both grades can be shipped in one container with separate packing and documentation.