GPC — GRAPHITIZED PETROLEUM COKE

Premium Carbon Raiser for Steel, Ductile Iron & Special Alloys  ·  Imported from China

## Section 1 — Hero content

GPC — Graphitized Petroleum Coke | Premium Carbon Raiser for Steel, Ductile Iron & Special Alloys

Sub-headline: Fixed Carbon ≥98.5–99.7%  ·  Sulphur ≤0.05%  ·  Nitrogen ≤0.03%  ·  Absorption rate 90–95%  ·  Sizes 0–30mm  ·  Imported from China

Single CTA: "Get a Quote / Request Sample COA"

Trust strip: ISO 9001  ·  SGS inspection available  ·  COA per lot  ·  REACH compliance  ·  Ex-stock India

## Section 2 — What is GPC?

Graphitized Petroleum Coke (GPC) is made from high-quality petroleum coke heated at 2,500–3,500°C in a graphitization furnace. This extreme heat restructures the carbon atoms into an ordered graphite crystal lattice — permanently transforming the material.

The result: ultra-high purity carbon with a graphite structure. Most impurities — sulphur, nitrogen, metal oxides — are vaporized during the process. What remains is the cleanest, most efficient carbon raiser available for steelmaking and foundry use.

In practical terms: fast carbon pickup, ultra-low sulphur and nitrogen, minimal ash and slag formation — consistent heat after heat.

## Section 3 — Full specifications (3 grades)

| Parameter | Premium GPC | Standard GPC | Economy GPC |
| --- | --- | --- | --- |
| Fixed Carbon (F.C.) % min | 99.5% | 98.5% | 98.0% |
| Sulphur (S) % max | 0.03% | 0.05% | 0.10% |
| Nitrogen (N) % max | 0.010% | 0.030% | 0.050% |
| Ash % max | 0.3% | 0.7% | 1.0% |
| Volatile Matter (VM) % max | 0.3% | 0.8% | 1.0% |
| Moisture % max | 0.3% | 0.5% | 0.5% |
| Graphitization degree | ≥98% | ≥95% | ≥90% |
| Absorption rate | 93–95% | 90–93% | 88–90% |
| Bulk density | 0.78–0.85 g/cc | 0.75–0.82 g/cc | 0.72–0.80 g/cc |
| Available sizes | 0–0.2mm · 0.2–1mm · 1–5mm · 3–8mm · 8–30mm | Same | Same |
| Colour | Black / dark grey with metallic lustre | Black | Black |
| Primary use | Ductile iron, special steel, ultra-low S/N applications | EAF/IF steelmaking, grey iron, general foundry | Cost-sensitive EAF, general carbon adjustment |

Note: 1–5mm is the most widely used size — balances fast dissolution with easy handling and minimal fines dust.

- COA per lot: F.C., S, N, Ash, VM, Moisture, size analysis — all parameters tested, not just F.C.

- Graphitization degree verified per lot — ask us for the test method used

## Section 4 — Why GPC is the preferred recarburizer

- Ultra-low sulphur (0.02–0.05%): reduces adverse effect on spheroidization and inoculation in ductile iron; prevents hot shortness in steel

- Ultra-low nitrogen (30–300 ppm): prevents sub-surface porosity and blowholes in ductile iron; prevents strain ageing in quality steel — no other carbon raiser matches GPC at this nitrogen level

- High absorption rate (90–95%): graphite crystal structure dissolves rapidly in molten iron — less material per heat, less slag, more predictable carbon pickup

- Improves nucleation in cast iron: graphite crystal nuclei promote nodule formation in ductile iron and improve graphite distribution in grey iron

- Reduces pig iron dependency: higher carbon recovery from scrap allows increased scrap steel usage, reducing pig iron in the charge

- Extends furnace lining life: clean dissolution, no slag — protects lining and reduces lining consumption over time

- Lower total cost: higher price per tonne offset by better recovery, reduced rework and tighter chemistry control heat to heat

## Section 5 — Applications

- EAF steelmaking: carbon trim additions after refining — hit target %C without pushing sulphur; quality steel, spring steel, bearing steel, tool steel

- Induction furnace steelmaking: added with charge or during melting; preferred by quality-conscious IF operators for consistent heat-to-heat chemistry

- Ductile iron / SG iron foundries: most critical application — S below 0.05% and N below 300 ppm essential for successful Mg treatment; GPC is the standard choice

- Grey iron foundries: stabilises carbon equivalent (CE), improves graphite morphology, improves machinability and surface finish of castings

- Special steel grades: stainless steel, bearing steel, tool steel, spring steel — all require strict S/N control that only GPC provides

- Precision and investment casting: consistent carbon control in high-value aerospace and automotive castings

## Section 6 — Buyer advantages

| Quality & consistency - Fixed plant source in China — same graphitization furnace, consistent lot to lot - Full COA: F.C., S, N, Ash, VM, Moisture, size analysis per lot - Graphitization degree verified — not all GPC in market is fully graphitized - SGS / Intertek pre-shipment inspection available on request - Reference sample retained 12 months per lot | Supply & commercial - All three GPC grades from one supplier — single point of contact - Standard 1–5mm always in stock at Indian port - Specialty sizes on 30–40 day import lead time - LCL from 500kg for trial orders - Competitive CIF / DAP pricing — contact us for current price |
| --- | --- |

Section 7 — Calling GPC Producers & Export Trading Companies

We are regular monthly importers with an active Indian buyer network — your material moves fast. We offer D/P or open account terms to qualified suppliers. Suppliers insisting on LC or full advance for every shipment find it hard to build volume in India — flexible payment terms is what makes a supply relationship work here.

What we need:

- F.C. ≥98.5% (SGS/BV COA) · S ≤0.05% · N ≤0.03% · Graphitization ≥95%

- Size: 1–5mm, ≥90% in range · Packing: 1MT jumbo bags

Send us: Company · Location · Monthly capacity · F.C./S/N % · FOB price

## Section 8 — Logistics

- Packaging: 25kg / 50kg bags in 1MT jumbo bags, or direct 1MT jumbo bags

- One 20-ft FCL: approx 22–23 MT of bagged GPC

- Ports: JNPT / Nhava Sheva (primary), Mundra, Hazira

- Transit from China: 15–20 days sea freight

- HS Code: 2713.12 (calcined petroleum coke) — GPC may also clear under 3801 depending on grade declaration

- Inland delivery to: Raipur / Chhattisgarh (EAF cluster) · Mandi Gobindgarh (IF cluster) · Muzaffarnagar · Rajkot · Coimbatore · Pune

- Lead time: ex-stock 3–7 days; fresh import 30–40 days from order

Frequently Asked Questions

Q1. What makes GPC different from calcined petroleum coke (CPC)?

GPC is graphitized at 2,500–3,500°C restructuring carbon into an ordered graphite lattice — giving S as low as 0.02–0.05% and absorption 90–95% vs CPC's 0.3–0.5% S and 80–90% absorption. GPC costs more per tonne but delivers better total value through higher recovery and cleaner melts.

Q2. What particle size of GPC should I use for my induction furnace?

1–5mm is standard for induction furnaces — fast dissolution without dust loss. For ladle trim additions, 0.2–1mm gives faster dissolution; avoid sizes above 8mm in IF as they dissolve too slowly before tapping.

Q3. My ductile iron castings have porosity — can GPC help?

Porosity in ductile iron is most commonly caused by excess nitrogen — switching from anthracite or CPC to premium GPC (N ≤0.010%) is frequently the fastest fix. GPC also improves nodule count through its graphite crystal nucleation effect.

Q4. What is absorption rate and why does it matter commercially?

Absorption rate is the percentage of added carbon that actually reaches the melt — GPC's 90–95% vs anthracite's 75–85% means significantly less material per heat. Always calculate cost per unit of carbon delivered, not cost per tonne purchased.

Q5. Can I get a sample and COA before placing a bulk order?

Yes — we dispatch 500g–1kg sample with COA (F.C., S, N, Ash, VM, Moisture, size analysis) within 3–5 days.

← Back to Carbon Raiser overview  ·  See also: Anthracite Coal  ·  Electrode Scrap